# Instructions For Decorating Wood & Papier Mache

Materials required:

Jo Sonja’s All Purpose Sealer (APS)

Background Paint Colour 
Jo Sonja’s Décor Crackle

Jo Sonja's Crackle Medium

Serviettes                
Sponges/ soft brush

Start by preparing the background colour for the wood. You can buy the background colours ready mixed or you can make your own colour using the white as your base and adding small amounts of the artist colours to achieve the desired effect.

Mix the paint with APS approx ratio 2:1 and apply to the wood. The APS helps give a better cover to the wood without soaking too far into it. You can apply the paint with either a sponge or a brush, as is your choice. Leave to dry.

Once dry apply a coat of Décor Crackle to the area that you would like cracked. Load your brush well with the medium and let it flow off of the brush.

DO NOT WORK THE DECOR CRACKLE TOO MUCH.

It must flow off of the brush and leave a good layer where required. You get bigger and better cracks if the medium is a thicker layer but if you work the medium too much it with not activate.

Once the Decor Crackle is dry you can apply a contrasting top coat of paint. Again do not over work the paint. Get in, get out. If you over work it you will stop the cracking process.

When choosing your top coat colour, please be aware that the crackle will not work if a metallic paint is used (ie Gold) or a iridescent/pearl paint.

The drying of the base coat of paint and crackle layer can be speeded up with a gentle hairdryer. Preferably the top coat must be left to dry naturally.

If you wish to speed up the drying time for the top layer, you can use the hairdryer, but you will then need to apply a coat of Crackle Medium (different to Decor Crackle) to get the best crackle effect.

The time between putting the décor crackle on and applying the top coat is recommended as ‘up to 6 hours’ when drying naturally, but I have before left it for up to a week and the crackle has still worked. If uncertain, try it.

You will get a different crackle effect according to how you apply the top paint. A sponge will give you a random crackle, a brush will give you a bark effect. Play and enjoy. Try it out on mirror board or scraps of mountboard to find out the different effects.

If you would like to apply napkins after you have finished crackling:-

Separate the tissues into the fine layers. Tear the tissue to give you the patterns that you wish to use. A torn edge makes it easier to blend the pieces together.

Apply the torn tissue to your project using the All Purpose Medium. Lay the tissue flat where you would like it to be. Load the brush well with the medium and, with soft strokes, apply the medium to the tissue - working from the centre of the piece outwards. Ensure that plenty of medium is applied.

If the tissue seems to be tearing it usually means that not enough medium is being used or the brush is being used too harshly - keep the brush flat and let it glide across the tissue.

If you want to varnish your piece, make sure you leave it for at least a couple of weeks in case you re activate the crackle medium and it cracks your varnish.